## Slide 1: Thermal stresses : probelms

## Slide 2: Problem 1

## Slide 3: Problem 1
Length = Ls=Lc=L= 1.2 m for both concrete and steel
Ac=a2,a=200mm
As=nxpxr2=, r= 9mm
n = no of rods = 18
Temperature rise =DT=27oC

## Slide 4: Problem 1
Whichever material expands more will have its expansion inhibited by the other.
In this case steel rods will tends to expand more and will try to pull the concrete along with it, while the concrete will try to restrict the expansion of the steel
So steel rods will see a compressive axial force F, while the concrete will see a tensile F.
Note that this F is the total force in the steel rods. Each rod sees F/n.
This is a literary statement of the force equilibrium equation Fs+Fc=0 or Fs=-Fc=F

## Slide 5: Problem 1
Thus the net expansion of steel rods will have two components
Expansion due to temperature
Expansion (negative and hence compression actually) due to the axial compressive force

## Slide 6: Problem 1
The net expansion of concrete will also have two components
Expansion due to temperature
Expansion due to the axial tensile force

## Slide 7: Problem 1
The geometrical constraint is that after the temperature stabilizes both steel and concrete rods must have the same length.
Thus

## Slide 8: Problem 1
We can now get F by solving this equation

## Slide 9: Problem 1
Once F is obtained the stresses in each individual component can be easily found out

## Slide 10: Problem 1
What is another way of looking at this problem ?
We have a steel rod and a concrete rod both having the same length. They are both subjected to the same rise in temperature while being acted upon by a force. If the change in length is same in both cases, what is the relation between the forces ? If the magnitude of the forces are same, find the magnitude of the forces and their nature for steel and concrete.

## Slide 11: Problem 2

## Slide 12: Problem 2
This problem is actually two problems rolled into one. Let us split the problem properly
1. What is the temperature rise required to close the gap between the rods ?
2. After the gap is bridged, what are the forces produced in the rods once the temperature settles down to 160 oC?

## Slide 13: Problem 2
C
D
First problem
We let s=0.5mm
This temperature rise will have to be deducted from the total rise in the second problem

## Slide 14: Problem 2
C
D
Second problem
The gap is now closed
C and D now coincide.
Let the temperature rise be DT2 for this part
All the forces generated will be due to DT2.

## Slide 15: Problem 2
C
D
We draw the FBD
This allows us to write the force equilibrium equation
We also note that will be two domains, AC and CB, since both area of cross section and material change at C.
RA
RA

## Slide 16: Problem 2
C
D
Domain AC
F(x)
RA
RA

## Slide 17: Problem 2
C
D
Domain CB
F(x)
RA
RA

## Slide 18: Problem 2
C
D
Domain CB
F(x)
RA
RA

## Slide 19: Problem 2
C
D
Displacement at B due to mechanical effects only

## Slide 20: Problem 2
Thermal expansion
C
D

## Slide 21: Problem 2
Geometrical constraint
Why is RHS=0 ?
Because all these expansions are not responsible for bridging the gap. That was due to the expansions calculated in part 1. These new expansions are responsible only for keeping the closed gap closed.
C
D

## Slide 22: Problem 2
Using the geometrical constraint we can get the reaction at A after the gap is closed.
C
D

## Slide 23: Problem 2
The force in the aluminium rod and the consequent stress is found from our analysis of domain AC
C
D

## Slide 24: Problem 2
The expansion of the Aluminium rod will have two parts, the free expansion from part 1 of the problem and the constrained expansion from part 2
C
D

## Slide 25: Problem 3
A rigid bar of weight W=340.5 kg hangs from three equally spaced wires, two of steel and one of aluminium. The diameter of the wires is 3.175 mm . Before they were loaded, all three wires had the same length. What temperature increase DT in all three wires will result in the entire load being carried by the steel wires? (Assume Es = 207 GPa, as = 11.7x10-6/°C, aal = 21.6x10-6/°C
W = 340.5 kg

## Slide 26: Problem 3
Let us assume all wires expand
We draw the FBD
We write down the equation of force equilibrium. Because of symmetry we do not need to consider the moment equation.
Taking moments about the center of the rigid bar simply tells us that both the steel wires have equal forces, which we can figure out anyway looking at the symmetry of the problem.
W = 340.5 kg
Fs
Fs
Fal

## Slide 27: Problem 3
Assuming expansion for all wires implies that both steel and aluminium wires are not loose. There is a possibility that one of them may not be in tension. We will need to check that once our problem is solved with this assumption. We will need to check if all the forces come out as positive with our chosen directions.
If any of them is negative it means that a wire being a wire and not a rod, will not be doing anything, and hence we will have to re do the problem assuming those wires are not there at all
W = 340.5 kg
Fs
Fs
Fal

## Slide 28: Problem 3
Expansion due to temperature. These will happen irrespective of whether the wire is loose or tight).
W = 340.5 kg
Fs
Fs
Fal

## Slide 29: Problem 3
Expansion due to forces (remember we need to check if these come out as negative)
W = 340.5 kg
Fs
Fs
Fal

## Slide 30: Problem 3
Because of the symmetry (both mechanical and thermal, all rods being heated equally), after heating the rigid bar has to be horizontal (Geometrical constraint)
Also both steel and aluminium wires have initial length of L and same area of cross section A. Hence
W
Fs
Fs
Fal

## Slide 31: Problem 3
We now combine use the force equilibrium equation and the constraint equation and solve them together
W = 340.5 kg
Fs
Fs
Fal

## Slide 32: Problem 3
We get the solution for the force in the aluminium and steel wires
W
Fs
Fs
Fal

## Slide 33: Problem 3
Since the aluminium wire must be carrying no force
W
Fs
Fs
Fal

## Slide 34: Problem 3
For this temperature rise, force in each steel wire can be directly obtained from the force equilibrium equations by setting the force in the aluminium wire as zero
We could have solved the problem by straight away starting with this value, but the idea was to not only solve this problem but get a more general understanding
W
Fs
Fs
Fal

## Slide 35: Problem 3
Once this problem is done using the numerical values, we can try redoing this problem by trying to find out what will happen for temperature rise below the answer obtained and above the answer obtained.
Our solutions will be valid for the first case, where the force in the aluminium wire will come out as positive indicating that the load is borne by all 3 wires
However the same expression will give a negative value for the second case. This indicates that beyond this temperature the aluminium wire will expand too much due to temperature and will become loose. Only the steel wires will carry the weight above this critical temperature rise and the expressions obtained by taking force in aluminium wire as zero will be valid beyond this point.

## Slide 36: Problem 4

## Slide 37: Problem 4
You may want to relook at this problem. The effect of tightening is now replaced by thermal expansion.

## Slide 38: Problem 4
In this case, comparing with the earlier problem we can now easily visualize that a temperature increase will cause the bolt with its lower thermal coefficient of expansion to expand less and hence pull at the sleeve from the inside trying to effectively compress it so that the lengths remain as close to equal as possible.
Thus the bolt will be under tension and the sleeve under compression.

## Slide 39: Problem 4
With our experience of the earlier problem we will not go into minute details of this problem, such as drawing of FBD of individual components.
We will simply state that the compressive force for the sleeve is F and the tensile force for the bolt is also F.

## Slide 40: Problem 4
Thermal expansion of sleeve
Expansion due to compressive force on sleeve
- sign is due to compression
Total change in length

## Slide 41: Problem 4
Thermal expansion of bolt
Expansion due to tensile force on bolt
+ sign is due to tension
Total change in length

## Slide 42: Problem 4
Geometric constraint is final lengths between the plates are same for both components.
Also initial lengths between the plates are same (L). Hence

## Slide 43: Problem 4
Solving

## Slide 44: Problem 4
Solving, we can get the required rise in temperature in terms of the force F and hence the stress in the bolt.

## Slide 45: Problem 5

## Slide 46: Problem 5
In this problem we have both prestressing (the act of tightening to introduce stresses in the contraption) as well as temperature change.
Note that there are two sleeves, outer and inner, joined by solder.
Also we will deal with shear strength of solder to keep the tubes joined together. This will help us understand how we can deal with shear stresses if screws or pins are used in place of solder or glue in certain problems.

## Slide 47: Problem 5
From our experience with previous problems we can now say without detailed FBDs that if the internal force at any transverse cross section of the bolt is F, the internal force for the the sleeve must be –F.

## Slide 48: Problem 5
From our experience with previous problems we can now say without detailed FBDs that if the internal force at any transverse cross section of the bolt is F, the internal force for the the sleeve must be –F.

## Slide 49: Problem 5
First consider the bolt
Length of bolt is
Area of cross section of the bolt is
Change in length due to force

## Slide 50: Problem 5
Bolt
Change in length due to change of temperature

## Slide 51: Problem 5
Bolt
Finally we know that the screw was turned to reduce the gap between the top and bottom plates.

## Slide 52: Problem 5
Bolt
Total change of length of the bolt

## Slide 53: Problem 5
Next consider the outer sleeve excluding the soldered part
Length of outer sleeve is
Area of cross section of outer sleeve is
Change in length due to force

## Slide 54: Problem 5
Outer sleeve
Change in length due to change of temperature

## Slide 55: Problem 5
Outer sleeve
Total change of length of the outer sleeve

## Slide 56: Problem 5
Next consider the soldered part. Note that we are ignoring the solder itself assuming it forms a very thin layer
Length of soldered part is s
Area of cross section of the soldered (jointed) part is
Change in length due to force

## Slide 57: Problem 5
Soldered part
Change in length due to change of temperature

## Slide 58: Problem 5
Soldered part
Total change of length of the soldered part

## Slide 59: Problem 5
Next consider the inner sleeve excluding the soldered part
Length of inner sleeve is
Area of cross section of inner sleeve is
Change in length due to force

## Slide 60: Problem 5
Inner sleeve
Change in length due to change of temperature

## Slide 61: Problem 5
Inner sleeve
Total change of length of the inner sleeve

## Slide 62: Problem 5
Geometrical constraint

## Slide 63: Problem 5
We can now get F

## Slide 64: Problem 5
The solder must resist this force F. In the solder this will show up as a shearing force between the two sleeves

## Slide 65: Problem 5
Suppose we had used N screws with radius r in place of the solder to keep the sleeves joined, with the material of the screw having same allowable shear stress. Then we could find out the number of screws required as shown below